## Slide 1: CH5715 Energy Conversion and Storage
http://jtsigroup.wp.st-andrews.ac.uk/ch5715-energy-conversion-and-storage/

## Slide 2
Impedance Spectroscopy
Introduction to EIS and process speciation

## Slide 3: Questions

## Slide 4: Electrode Processes

## Slide 9
Investigation of role of microstructure in fuel oxidation performance
Patrick Muhl
Introduction
ACC
Anode
Electrolyte
Cathode
CCC
air
H20
N2
H2

## Slide 10
Approach
Why do we care about diffusion/ concentration/ utilization - “losses” at the anode?
1. Even though they are mostly small, they are losses!
2. These losses are suspected to increase when using CH4!
3. Vital in the anode supported FC design!

## Slide 11
Patrick Muhl
Approach
Rs
Rp1
Rp2
Rtotal

## Slide 12
tacc >> tanode , telectrolyte
Patrick Muhl
Introduction
fuel
H20
Total current ≠ 0
H20 (CO, CO2) enriched reaction zone
Competition of H2 “getting in”, versus
H20 (CO2) “getting out”
Material properties
Thickness (diffusion length)
Porosity
Tortuosity
Density
Grain size
Gas properties
Diffusion coefficient
Binary or multiple molecules
Operation setup
Mass flows (i.e. mH2)
Temperature
Current density
.

## Slide 13: Solid Oxide Fuel Cells: Cathode Materials and Interfacial Reactions

## Slide 14
Nature of Three Phase Boundary

## Slide 16
Charge transfer

## Slide 23
kHz
Charge transfer
Hz
Diffusion

## Slide 24: Resume of impedance – process relations
CC
Electrode
O
R
Electrolyte
Mass transport
Warburg types
Charge transfer
Polarisation
R/C
Ion and electron
Transport
R/C